# Template stripped gold according to Sonia

Cleave mica – leave at vacuum and heat overnight at 400C

This gets rid of impurities (?) and it becomes possible to peel of the Au.

200-300nm of Au is deposited on mica at 10 Å/s.

The Au side of the evaporated mica is glued to 1x1cm squares of Si with Epoxy glue ("EPOTEK 301").

IMPORTANT: let the glue dry completely before the next step.

Then, with tweezers or a cutter, push on the glued Si piece,

horizontally until it comes off. Usually you have Au surface there, and

no mica is exposed.

I never got an answer to how she knows that there is no mica left on the Au after stripping.