## Slide 1
1 Freshly cleaved mica in water
OH-
OH-
OH-
OH-
OH-
OH-
Surface hydroxyl groups
Hydrophilic surface
2 Modification of mica with
ethanolamine
HO-C-C-NH2
HNH
C
C
O
Surface amine groups
Hydrophobic surface
Surface coverage: 500 per m2 or 1 per 45x45 nm2
4 Binding of a protein to succinimidyl
Spacer of about 1 nm
succ
Ref: Hinterdorfer, P. et al., PNAS 93, 3477-3481, 1996
Trau, M. et al., J. of Colloid and Interface Science 148-1, 1991
Lys (K)
3 Binding of succinimidyl to amine
succ
succ
NH2-
succ
4 nm
Si
Si
Si
Si
Si
Si
Si
Notes: The potassium ions (K+) are dissolved in water.
2. NH3+ in water

## Slide 2
2 Ethanolamine HO-C-C-NH2
and DMSO, overnight
Ref: Hinterdorfer, P. et al., PNAS 93, 3477-3481, 1996
Trau, M. et al., J. of Colloid and Interface Science 148-1, 1991
100 °C
3 Binding of succinimidyl to amine
Recipe:
Be careful, do not breath or spill these chemicals! Always use the acid hood!
Add molecular sieve beads to the DMSO bottle!
First make a solution of 6.6 g ethanolamine
in 12 ml DMSO and heat the solution to 70 ° C.
Add molecular sieve beads to this solution.
Cleave mica disks on two sides and insert them immediately in the solution.
Cover the beaker with aluminum foil and leave it like this overnight.
Now rinse the mica surfaces in hot DMSO (twice) and in ethanol, dry with nitrogen. The amine modified mica can be stored in a dessicator (HL702) for a few days, or used immediately for the next step:
Make a solution of 1 mg/ml ethylene glycol-bis-(succinimidyl-succinate) in chloroform containing 0.5% triethylamine (10 or 20 ml is enough, in 10 ml you insert 50 l triethylamine). Put the amine modified mica disks in the succinimidyl solution and leave them there for 1.5-3 hours. Then wash the mica in chloroform and dry with nitrogen.
Put 50 l of a pea lectin PSL solution of 1 ug/ml on the mica during two-four hours, remove the excess of PSL and rinse with buffer, leave a droplett of 75 l PBS on the mica. Your sample is ready for an AFM experiment.