consider (LaCa)MnO3 structure on  SrTiO3 as tetragonal with a-axis in the substrate plane and the c-axis perpendicular

wavelength =1.54060 Angstrom

L120 (LaCa)MnO3 on SrTiO3

<0 0 3> peak  of substrate at 72.562 deg (72.559 is theoretical value) , (2theta)

<0 0 3.>peak at 74.493 deg

<1 0 3> peak at 78.423 deg  then a=4.237 A and c= 3.820 A

<1 0 3> peak at 78.720 deg  then a=4.083 A and c= 3.820 A

These values seem nonsense

Other model: It appeared that for measuring   the < 0 1 3> and <0 2 3> reflections,  alignment of the film is essential and that alignment according to the <01 3> and <0 2 3> reflections of the substrate is not sufficient. In the case of this film the misorientation of the  film with respect of the substrate is >0.2 degrees (theta).

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.296     23.294      0.002

0  0  2     47.624     47.627     -0.003

0  0  3     74.528     74.551     -0.023

0  1  3     79.135     79.136     -0.001

0  2  3     92.589     92.594     -0.005

a= 3.9028 +/- 0.0039 A;

c= 3.8156 +/- 0.0004 A

peak widths

L120 FWHM <0 0 1> peak         = 0.076 degrees

L120 FWHM <0 0 2> peak         = 0.077 degrees

L120 FWHM <0 0 3> peak         = 0.096 degrees

L120 FWHM <0 1 3> peak         = 0.111 degrees

L120 FWHM <0 2 3> peak         = 0.121 degrees

L120 FWHM <0 0 2> rock curve   = 0.058 degrees (multiple peaks)

L120 FWHM <0 1 3> rock curve   = 0.043 degrees

L120 FWHM <0 2 3> rock curve   = 0.053 degrees

L133 (LaCa)MnO3 on NdGaO3  <1 1 0> (NdGaO3: a,b=3.863 A, c=3.854 A)

From  fringe pattern on shoulder <2 2 0> substrate peak, film is visible d=50.7 +/-1.2 nm

L152 (LaCa)MnO3 on SrTiO3

consider (LaCa)MnO3 structure on  SrTiO3 as tetragonal with a-axis in the substrate plane and the c-axis perpendicular

<0 0 3> peak  of substrate at 72.562 deg (72.559 is theoretical value) , (2theta)

<0 0 3.>peak at 74.493 deg

<1 0 3> peak at 78.826 deg

then a=4.016 A and c= 3.818 A

Other model: It appeared that for measuring   the < 0 1 3> and <0 2 3> reflections,  alignment of the film is essential and that alignment according to the <01 3> and <0 2 3> reflections of the substrate is not sufficient. In the case of this film the misorientation of the  film with respect of the substrate is >0.1 degrees (theta).

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.244     23.275     -0.031

0  0  2     47.570     47.586     -0.016

0  0  3     74.460     74.480     -0.020

1  0  3     79.097     79.096      0.001

2  0  3     92.645     92.640      0.005

a= 3.8904 +/- 0.0025 A;

c= 3.8187 +/- 0.0003 A

L154 (LaCa)MnO3 on SrTiO3

h  k  l     2th meas.  2th calc. diff.

0  0  1     23.199     23.198      0.001

0  0  2     47.438     47.422      0.016

0  0  3     74.226     74.197      0.029

1  0  3     78.784     78.784      0.000

2  0  3     92.232     92.231      0.001

a= 3.9053 +/- 0.0044 A;

c= 3.8311 +/- 0.0004 A

L161 (LaCa)MnO3 on SrTiO3

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.305     23.311     -0.006

0  0  2     47.645     47.664     -0.019

0  0  3     74.588     74.614     -0.026

1  0  3     79.204     79.204      0.000

2  0  3     92.676     92.674      0.002

a= 3.9007 +/- 0.0038 A;

c= 3.8128 +/- 0.0004 A

peak widths

L161 FWHM <0 0 1> peak         = 0.242 degrees   fast growth

L161 FWHM <0 0 2> peak         = 0.258 degrees

L161 FWHM <0 0 3> peak         = 0.310 degrees

L161 FWHM <0 1 3> peak         = 0.203 degrees

L161 FWHM <0 2 3> peak         = 0.203 degrees

L161 FWHM <0 0 1> rock curve   = 0.034 degrees

L161 FWHM <0 0 2> rock curve   = 0.048 degrees

L161 FWHM <0 0 3> rock curve   = 0.039 degrees

L161 FWHM <1 0 3> rock curve   = 0.037 degrees

L161 FWHM <2 0 3> rock curve   = 0.068 degrees

L162 (LaCa)MnO3 on SrTiO3  (d=38.7 nm)

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.232     23.246     -0.014

0  0  2     47.501     47.525     -0.024

0  0  3     74.327     74.373     -0.046

0  1  3     78.950     78.950     -0.000

0  2  3     92.375     92.377     -0.002

a= 3.9079 +/- 0.0070 A;

c= 3.8234 +/- 0.0007 A

L162 FWHM <0 0 1> peak         = 0.223 degrees   slow growth

L162 FWHM <0 0 2> peak         = 0.228 degrees

L162 FWHM <0 0 3> peak         = 0.259 degrees

L162 FWHM <0 1 3> peak         = 0.159 degrees

L162 FWHM <0 2 3> peak         = 0.153 degrees

L162 FWHM <0 0 1> rock curve   = 0.029 degrees

L162 FWHM <0 0 2> rock curve   = 0.029 degrees

L162 FWHM <0 0 3> rock curve   = 0.029 degrees

L162 FWHM <1 0 3> rock curve   = 0.035 degrees

L162 FWHM <2 0 3> rock curve   = 0.049 degrees

L165 (LaCa)MnO3 on SrTiO3

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.211     23.256     -0.045

0  0  2     47.536     47.545     -0.009

0  0  3     74.418     74.409      0.009

1  0  3     78.977     78.974      0.003

2  0  3     92.379     92.367      0.012

a= 3.9126 +/- 0.0024 A;

c= 3.8218 +/- 0.0001 A

L168 (LaCa)MnO3 on SrTiO3

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.235     23.237     -0.002

0  0  2     47.508     47.504      0.004

0  0  3     74.333     74.338     -0.005

1  0  3     78.922     78.923     -0.001

2  0  3     92.366     92.369     -0.003

a= 3.9050 +/- 0.0013 A;

c= 3.8249 +/- 0.0001 A

L172 (LaCa)MnO3 on SrTiO3

With aligment according to <0 1 3> reflection of substrate n <0 1 3) reflection of film was found.

However, new measurement , alignment of film for <0 1 3> and <0 2 3> reflections

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.315     23.307      0.008

0  0  2     47.656     47.654      0.002

0  0  3     74.591     74.597     -0.006

1  0  3     79.170     79.171     -0.001

2  0  3     92.592     92.595     -0.003

a= 3.9075 +/- 0.0012 A;

c= 3.8136 +/- 0.0001 A

L174 (LaCa)MnO3 on SrTiO3

tetragonal model seems to work.:

<0 0 2> peak at 47.137 deg (2theta)

<0 0 3.>peak at 73.651 deg

<1 0 3> peak at 78.283 deg

then a=3.883 A and c= 3.861 A

however, new measurement , alignment of film for <0 1 3> and <0 2 3> reflections

h  k  l     2th meas.  2th calc.   diff.

0  0  2     47.108     47.152     -0.044

0  0  3     73.638     73.675     -0.037

0  1  3     78.275     78.357     -0.082

0  2  3     91.964     92.061     -0.097

a= 3.8697 +/- 0.0061 A;

c= 3.8580 +/- 0.0008 A

another attempt

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.039     23.037      0.002

0  0  2     47.087     47.077      0.010

0  0  3     73.626     73.603      0.023

0  1  3     78.268     78.268      0.000

0  2  3     91.923     91.921      0.002

a= 3.8769 +/- 0.0035 A;

c= 3.8577 +/- 0.0004 A

peak widths

L174 FWHM <0 0 1> peak         = 0.093 degrees

L174 FWHM <0 0 2> peak         = 0.175 degrees

L174 FWHM <0 0 3> peak         = 0.274 degrees

L174 FWHM <0 1 3> peak         = 0.225 degrees

L174 FWHM <0 2 3> peak         = 0.295 degrees

L174 FWHM <0 0 1> rock curve   = 0.149 degrees

L174 FWHM <0 0 2> rock curve   = 0.171 degrees

L174 FWHM <0 0 3> rock curve   = 0.167 degrees

L174 FWHM <1 0 3> rock curve   = 0.198 degrees

L174 FWHM <2 0 3> rock curve   = 0.229 degrees

L178 substrate SrTiO3

h  k  l     2th meas.  2th calc.   diff.

0  0  1     22.773     22.772      0.001

0  0  2     46.490     46.494     -0.004

0  0  3     72.582     72.592     -0.010

1  0  3     77.220     77.213      0.007

c= 3.9046 +/- 0.0007 A;

L178 film

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.248     23.249     -0.001

0  0  2     47.501     47.498      0.003

0  0  3     74.306     74.306     -0.000

1  0  3     78.880     78.881     -0.001

a= 3.9095 +/- 0.0013 A;

c= 3.8276 +/- 0.0000 A;

L188 SrTiO3 substrate

h  k  l     2th meas.  2th calc.   diff.

0  0  1     22.772     22.771      0.001

0  0  2     46.483     46.482      0.001

0  0  3     72.538     72.566     -0.028

1  0  3     77.183     77.184     -0.001

2  0  3     90.668     90.659      0.009

a= 3.9062 +/- 0.0011 A;

L188 film (on SrTiO3)

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.228     23.256     -0.028

1  0  2     53.405     53.329      0.076

0  0  2     47.469     47.475     -0.006

1  0  3     78.883     78.878      0.005

0  0  3     74.244     74.244     -0.000

2  0  3     92.453     92.463     -0.010

a= 3.8852 +/- 0.0031 A;

c= 3.8318 +/- 0.0001 A;

L188 annealed in vacuum; substrate

h  k  l     2th meas.  2th calc.   diff.

0  0  1     22.818     22.818      0.000

0  0  2     46.521     46.527     -0.006

0  0  3     72.582     72.609     -0.027

1  0  3     77.224     77.226     -0.002

2  0  3     90.707     90.701      0.006

a= 3.9064 +/- 0.0010 A;

FWHM <0 0 1> rock curve   = 0.048 degrees

FWHM <0 0 2> rock curve   = 0.052 degrees

FWHM <0 0 3> rock curve   = 0.057 degrees

FWHM <1 0 3> rock curve   = 0.061 degrees

FWHM <2 0 3> rock curve   = 0.058 degrees

film annealed

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.223     23.223     -0.000

0  0  2     47.422     47.417      0.005

1  0  3     78.731     78.759     -0.028

0  0  3     74.150     74.150      0.000

2  0  3     92.285     92.270      0.015

a= 3.8962 +/- 0.0038 A;

c= 3.8355 +/- 0.0000 A;

FWHM <0 0 1> rock curve   = 0.206 degrees

FWHM <0 0 2> rock curve   = 0.276 degrees

FWHM <0 0 3> rock curve   = 0.219 degrees

FWHM <1 0 3> rock curve   = 0.209 degrees

FWHM <2 0 3> rock curve   = 0.172 degrees

188 after 2nd annealing in vacuum

substrate

h  k  l     2th meas.  2th calc.   diff.

0  0  1     22.776     22.782     -0.006

0  0  2     46.513     46.497      0.016

0  0  3     72.590     72.588      0.002

1  0  3     77.196     77.207     -0.011

2  0  3     90.697     90.688      0.009

a= 3.9054 +/- 0.0007 A;

film after 2nd annealing in vacuum

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.183     23.190     -0.007

0  0  2     47.392     47.372      0.020

1  0  3     78.666     78.701     -0.035

0  0  3     74.091     74.091      0.000

2  0  3     92.233     92.215      0.018

a= 3.8959 +/- 0.0055 A;

c= 3.8371 +/- 0.0001 A;

FWHM <0 0 1> rock curve   = 0.190 degrees

FWHM <0 0 2> rock curve   = 0.188 degrees

FWHM <0 0 3> rock curve   = 0.058 degrees

FWHM <1 0 3> rock curve   = 0.067 degrees

L188 after annealing in air + vacuum

substrate

h  k  l     2th meas.  2th calc.   diff.

0  0  1     22.757     22.768     -0.011

0  0  2     46.490     46.473      0.017

0  0  3     72.577     72.550      0.027

1  0  3     77.181     77.166      0.015

2  0  3     90.625     90.637     -0.012

a= 3.9070 +/- 0.0012 A;

cellvolume=  59.64 +/-   0.03 A^3

film

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.219     23.231     -0.012

0  0  2     47.493     47.474      0.019

0  0  3     74.280     74.276      0.004

1  0  3     78.879     78.880     -0.001

2  0  3     92.377     92.383     -0.006

a= 3.8970 +/- 0.0020 A;

c= 3.8283 +/- 0.0001 A;

FWHM <0 0 1> rock curve   = 0.212 degrees

FWHM <0 0 2> rock curve   = 0.231 degrees

FWHM <0 0 3> rock curve   = 0.253 degrees

FWHM <1 0 3> rock curve   = 0.262 degrees

FWHM <2 0 3> rock curve   = 0.321 degrees

NdGaO3 <1 1 0> substrate, without film

h  k  l     2th meas.  2th calc.   diff.

1  0  1     33.021     33.018      0.003

1  0  2     53.301     53.260      0.041

2  0  2     69.201     69.241     -0.040

1  0  3     78.586     78.595     -0.009

2  0  3     92.681     92.634      0.047

a= 3.8222 +/- 0.0055 A;

c= 3.8497 +/- 0.0018 A

L189 (LaCa)MnO3 on NdGaO3 <1 1 0>

h  k  l     2th meas.  2th calc.   diff.

1  0  1     33.016     33.015      0.001

1  0  2     53.308     53.259      0.049

2  0  2     69.199     69.241     -0.042

1  0  3     78.586     78.596     -0.010

2  0  3     92.686     92.637      0.049

a= 3.8219 +/- 0.0059 A;

c= 3.8494 +/- 0.0021 A

cellvolume=  56.23 +/-   0.13 A^3

film

h  k  l     2th meas.  2th calc.   diff.

1  0  1     32.832     32.785      0.047

2  0  2     68.734     68.707      0.027

a= 3.8617 +/- 0.0000 A;

L190 substrate NdGaO3 <1 1 0>

h  k  l     2th meas.  2th calc.   diff.

1  0  1     33.055     33.020      0.035

2  0  2     69.244     69.259     -0.015

1  0  2     53.228     53.265     -0.037

1  0  3     78.628     78.607      0.021

2  0  3     92.687     92.660      0.027

a= 3.8203 +/- 0.0049 A;

c= 3.8489 +/- 0.0017 A;

L190 film

h  k  l     2th meas.  2th calc.   diff.

1  0  1     32.952     32.955     -0.003

2  0  2     69.026     69.027     -0.001

a= 3.8487 +/- 0.0000 A;

L190 after annealing in vacuum

Substrate:

h  k  l     2th meas.  2th calc.   diff.

1  0  1     33.022     33.045     -0.023

2  0  2     69.211     69.303     -0.092

1  0  2     53.312     53.279      0.033

1  0  3     78.584     78.612     -0.026

2  0  3     92.686     92.694     -0.008

a= 3.8163 +/- 0.0080 A;

c= 3.8496 +/- 0.0028 A;

film:

h  k  l     2th meas.  2th calc.   diff.

1  0  1     32.882     32.860      0.022

1  0  3     78.405     78.445     -0.040

2  0  2     68.805     68.808     -0.003

2  0  3     92.240     92.181      0.059

a= 3.8649 +/- 0.0037 A;

c= 3.8540 +/- 0.0027 A

L190 after 2nd annealing

Substrate

h  k  l     2th meas.  2th calc.   diff.

1  0  1     32.992     32.978      0.014

1  0  2     53.250     53.228      0.022

1  0  3     78.526     78.569     -0.043

2  0  2     69.177     69.182     -0.005

2  0  3     92.641     92.582      0.059

a= 3.8257 +/- 0.0048 A;

c= 3.8493 +/- 0.0027 A;

film

h  k  l     2th meas.  2th calc.   diff.

1  0  1     32.852     32.852     -0.000

2  0  2     68.779     68.779     -0.000

a= 3.8612 +/- 0.0000 A;

L190 after annealing  in air/ vacuum

substrate

h  k  l     2th meas.  2th calc.   diff.

1  0  1     33.020     32.993      0.027

1  0  2     53.244     53.249     -0.005

1  0  3     78.554     78.596     -0.042

2  0  2     69.194     69.196     -0.002

2  0  3     92.664     92.603      0.061

a= 3.8264 +/- 0.0034 A;

c= 3.8487 +/- 0.0027 A; cellvolume=  56.35 +/-   0.08 A^3

FWHM <2 0 2> rocking curve   = 0.044 degrees

film

h  k  l     2th meas.  2th calc.   diff.

1  0  1     32.877     32.877     -0.000

2  0  2     68.893     68.893     -0.000

a= 3.8536 +/- 0.0000 A;  cellvolume=  57.22 +/-   0.00 A^3

FWHM <2 0 2> rocking curve   = 0.057 degrees

L191

substrate

h  k  l     2th meas.  2th calc.   diff.

0  0  1     22.782     22.782     -0.000

0  0  2     46.504     46.506     -0.002

0  0  3     72.596     72.608     -0.012

1  0  3     77.234     77.229      0.005

2  0  3     90.718     90.718      0.000;

a= 3.9042 +/- 0.0005 A;

film

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.273     23.270      0.003

0  0  2     47.576     47.586     -0.010

0  0  3     74.453     74.486     -0.033

1  0  3     79.075     79.076     -0.001

2  0  3     92.542     92.547     -0.005

a= 3.9010 +/- 0.0053 A;

c= 3.8181 +/- 0.0005 A;  cellvolume=  58.10 +/-   0.11 A^3

substrate

FWHM <0 0 1> rock curve   = 0.112 degrees

FWHM <0 0 2> rock curve   = 0.110 degrees

FWHM <0 0 3> rock curve   = 0.095 degrees

FWHM <1 0 3> rock curve   = 0.069 degrees

FWHM <2 0 3> rock curve   = 0.089 degrees

film

FWHM <0 0 1> rock curve   = 0.196 degrees

FWHM <0 0 2> rock curve   = 0.193 degrees

FWHM <0 0 3> rock curve   = 0.172 degrees

FWHM <1 0 3> rock curve   = 0.188 degrees

FWHM <2 0 3> rock curve   = 0.238 degrees

L192

Substrate

h  k  l     2th meas.  2th calc.   diff.

0  0  1     22.773     22.776     -0.003

0  0  2     46.496     46.491      0.005

0  0  3     72.577     72.581     -0.004

1  0  3     77.193     77.200     -0.007

2  0  3     90.686     90.681      0.005

a= 3.9055 +/- 0.0004 A;

film

FWHM <0 0 1> rock curve   = 0.064 degrees

FWHM <0 0 2> rock curve   = 0.059 degrees

FWHM <0 0 3> rock curve   = 0.040 degrees

FWHM <1 0 3> rock curve   = 0.060 degrees

FWHM <2 0 3> rock curve   = 0.079 degrees

Film

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.353     23.359     -0.006

0  0  2     47.734     47.728      0.006

0  0  3     74.683     74.699     -0.016

1  0  3     79.287     79.289     -0.002

2  0  3     92.756     92.763     -0.007

a= 3.9002 +/- 0.0033 A;

c= 3.8106 +/- 0.0002 A ;  cellvolume=  57.96 +/-   0.07 A^3

FWHM <0 0 1> rock curve   = 0.074 degrees

FWHM <0 0 2> rock curve   = 0.074 degrees

FWHM <0 0 3> rock curve   = 0.077 degrees

FWHM <1 0 3> rock curve   = 0.093 degrees

FWHM <2 0 3> rock curve   = 0.128 degrees

LCMO01 15-9-2005

d=24.50 nm

Substrate

h  k  l     2th meas.  2th calc.   diff.

0  0  1     22.786     22.822     -0.036

0  0  2     46.549     46.529      0.020

0  0  3     72.630     72.608      0.022

1  0  3     77.236     77.225      0.011

2  0  3     90.679     90.697     -0.018

a=  3.9067 +/-  0.0014 Angstrom

FWHM <0 0 1>     = 0.043 degrees

FWHM <0 0 2>     = 0.070 degrees

FWHM <0 0 3>     = 0.076 degrees

FWHM <1 0 3>     = 0.091 degrees

FWHM <2 0 3>     = 0.089 degrees

FWHM <0 0 1> rock curve   = 0.037 degrees

FWHM <0 0 2> rock curve   = 0.039 degrees

FWHM <0 0 3> rock curve   = 0.031 degrees

film

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.235     23.248     -0.013

0  0  2     47.537     47.535      0.002

0  0  3     74.384     74.395     -0.011

1  0  3     78.977     78.978     -0.001

2  0  3     92.418     92.421     -0.003

a=  3.9053 +/-  0.0022 Angstrom, c=  3.8221 +/-  0.0002 Angstrom

FWHM <0 0 1>     = 0.336 degrees

FWHM <0 0 2>     = 0.406 degrees

FWHM <0 0 3>     = 0.451 degrees

FWHM <1 0 3>     = 0.218 degrees

FWHM <2 0 3>     = 0.170 degrees

FWHM <0 0 1> rock curve   = 0.046 degrees

FWHM <0 0 2> rock curve   = 0.040 degrees

FWHM <0 0 3> rock curve   = 0.044 degrees

LCMO02 28-9-2005

Substrate

h  k  l     2th meas.  2th calc.   diff.

0  0  1     22.766     22.794     -0.028

0  0  2     46.504     46.495      0.009

0  0  3     72.584     72.566      0.018

1  0  3     77.206     77.181      0.025

2  0  3     90.624     90.648     -0.024

a=  3.9076 +/-  0.0016 Angstrom,

FWHM <0 0 1>     = 0.065 degrees

FWHM <0 0 2>     = 0.078 degrees

FWHM <0 0 3>     = 0.070 degrees

FWHM <1 0 3>     = 0.092 degrees

FWHM <2 0 3>     = 0.118 degrees

FWHM <0 0 1> rock curve   = 0.069 degrees

FWHM <0 0 2> rock curve   = 0.057 degrees

FWHM <0 0 3> rock curve   = 0.079 degrees

FWHM <1 0 3> rock curve   = 0.054 degrees

FWHM <2 0 3> rock curve   = 0.038 degrees

film

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.317     23.348     -0.031

0  0  2     47.663     47.633      0.030

0  0  3     74.589     74.492      0.097

1  0  2     53.449     53.418      0.031

1  0  3     79.073     79.074     -0.001

2  0  3     92.511     92.515     -0.004

a=  3.9056 +/-  0.0050 Angstrom,

c=  3.8224 +/-  0.0012 Angstrom

FWHM <0 0 1>     = 0.191 degrees

FWHM <0 0 2>     = 0.242 degrees

FWHM <0 0 3>     = 0.337 degrees

FWHM <1 0 2>     =       degrees

FWHM <1 0 3>     = 0.294 degrees

FWHM <2 0 3>     = 0.383 degrees

FWHM <0 0 1> rock curve   = 0.077 degrees

FWHM <0 0 2> rock curve   = 0.087 degrees

FWHM <0 0 3> rock curve   = 0.110 degrees

FWHM <1 0 3> rock curve   = 0.130 degrees

FWHM <2 0 3> rock curve   = 0.133 degrees

L208-1 (LaCa)MnO3 on SrTiO3

Substrate

h  k  l     2th meas.  2th calc.   diff.

0  0  1     22.762     22.747      0.015

0  0  2     46.499     46.458      0.041

0  0  3     72.579     72.543      0.036

1  0  3     77.207     77.161      0.046

2  0  3     90.658     90.637      0.021

a=  3.9061 +/-  0.0003 Angstrom,

FWHM <0 0 1>     = 0.065 degrees (2theta)

FWHM <0 0 2>     = 0.069 degrees

FWHM <0 0 3>     = 0.081 degrees

FWHM <1 0 3>     = 0.081 degrees

FWHM <2 0 3>     = 0.092 degrees

FWHM <0 0 1> rock curve   = 0.052 degrees (theta)

FWHM <0 0 2> rock curve   = 0.053 degrees

FWHM <0 0 3> rock curve   = 0.057 degrees

FWHM <1 0 3> rock curve   = 0.056 degrees

FWHM <2 0 3> rock curve   = -     degrees

film

h  k  l     2th meas.  2th calc.   diff.

0  0  1     23.334     23.316      0.018

0  0  2     47.658     47.645      0.013

1  0  2     53.458     53.436      0.022

0  0  3     74.591     74.564      0.027

1  0  3     79.114     79.152     -0.038

2  0  3     92.577     92.619     -0.042

a=  3.9015 +/-  0.0075 Angstrom

c=  3.8161 +/-  0.0013 Angstrom

FWHM <0 0 1>     = 0.176 degrees (2theta)

FWHM <0 0 2>     = 0.224 degrees

FWHM <0 0 3>     = 0.308 degrees

FWHM <1 0 2>     = 0.285 degrees

FWHM <1 0 3>     = 0.307 degrees

FWHM <2 0 3>     = 0.298 degrees

FWHM <0 0 1> rock curve   = 0.068 degrees (theta)

FWHM <0 0 2> rock curve   = 0.113 degrees

FWHM <0 0 3> rock curve   = 0.161 degrees

FWHM <0 0 3> rock curve   = 0.161 degrees

FWHM <1 0 2> rock curve   = 0.285 degrees

FWHM <2 0 3> rock curve   = -     degrees

L316 (LaCa)MnO3 on SrTiO3

h  k  l 2th-meas  2th-cal   diff.

0  0  1  22.7980  22.7420   0.0560

0  0  2  46.4880  46.4474   0.0406

0  0  3  72.5720  72.5246   0.0474

1  0  3  77.1990  77.1411   0.0579

2  0  3  90.6520  90.6121   0.0399

FWHM <0 0 1>     = 0.056 degrees (2theta)

FWHM <0 0 2>     = 0.074 degrees

FWHM <0 0 3>     = 0.079 degrees

FWHM <1 0 3>     = 0.097 degrees

FWHM <2 0 3>     = 0.098 degrees

FWHM <0 0 1> rock curve   = 0.044 degrees (theta)

FWHM <0 0 2> rock curve   = 0.042 degrees

FWHM <0 0 3> rock curve   = 0.034 degrees

FWHM <1 0 3> rock curve   = 0.045 degrees

FWHM <2 0 3> rock curve   = 0.044 degrees

a=  3.9070 +/-  0.0010 Angstrom,

h  k  l 2th-meas  2th-cal   diff.

0  0  1  23.3030  23.3288  -0.0258

0  0  2  47.6540  47.7017  -0.0477

0  0  3  74.6040  74.6789  -0.0749

1  0  3  79.2730  79.2767  -0.0037

2  0  3  92.7850  92.7752   0.0098

a=  3.8965 +/-  0.0146 Angstrom,

c=  3.8100 +/-  0.0014 Angstrom

FWHM <0 0 1>     = 0.230 degrees (2theta)

FWHM <0 0 2>     = 0.278 degrees

FWHM <0 0 3>     = 0.404 degrees

FWHM <1 0 3>     = 0.349 degrees

FWHM <2 0 3>     = 0.427 degrees

FWHM <0 0 1> rock curve   = 0.051 degrees (theta)

FWHM <0 0 2> rock curve   = 0.059 degrees

FWHM <0 0 3> rock curve   = 0.073 degrees

FWHM <1 0 3> rock curve   = 0.186 degrees

FWHM <2 0 3> rock curve   = 0.290 degrees

L400 (LaCa)MnO3 on SrTiO3 (Ivan) d= 15.6 nm

Substrate

h  k  l 2th-meas  2th-cal   diff.

0  0  1  22.7670  22.7516   0.0154

0  0  2  46.5070  46.4679   0.0391

1  0  3  77.2090  77.1792   0.0298

2  0  3  90.6660  90.6604   0.0056

a=  3.9053 +/-  0.0005 Angstrom,

<001> FWHM= 0.056 degrees (2theta)

<002> FWHM= 0.069 degrees

<003> FWHM= 0.000 degrees

<103> FWHM= 0.097 degrees

<203> FWHM= 0.090 degrees

rocking curves

<001> FWHM= 0.039 degrees (theta)

<002> FWHM= 0.039 degrees

<103> FWHM= 0.042 degrees

<203> FWHM= 0.041 degrees

film

h  k  l 2th-meas  2th-cal   diff.

0  0  1  23.3950  23.3812   0.0138

0  0  2  47.8980  47.8141   0.0839

1  0  2  53.6730  53.5818   0.0912

1  0  3  79.5010  79.4497   0.0513

2  0  3  92.9230  92.8944   0.0286

a=  3.9040 +/-  0.0087 Angstrom,

c=  3.8016 +/-  0.0008 Angstrom

<001> FWHM= 0.458 degrees (2theta)

<002> FWHM= 0.613 degrees

<102> FWHM= 0.183 degrees

<103> FWHM= 0.367 degrees

<203> FWHM= 0.348 degrees

rocking curves

<001> FWHM= 0.050 degrees (theta)

<002> FWHM= 0.051 degrees

<102> FWHM= 0.085 degrees

<103> FWHM= 0.084 degrees

<203> FWHM= 0.092 degrees

h  k  l 2th-meas  2th-cal   diff.

0  0  1  23.3230  23.3317  -0.0087

0  0  2  47.7040  47.7080  -0.0040

0  0  3  74.6790  74.6897  -0.0107

1  0  3  79.2620  79.2626  -0.0006

2  0  3  92.6900  92.6887   0.0013

L406 (LaCa)MnO3 on SrTiO3 (Ivan) d= 21.5 nm

Substrate

h  k  l 2th-meas  2th-cal   diff.

0  0  1  22.7720  22.7471   0.0249

0  0  2  46.5090  46.4583   0.0507

0  0  3  72.5870  72.5432   0.0438

1  0  3  77.2290  77.1613   0.0677

2  0  3  90.6600  90.6378   0.0222

a=  3.9061 +/-  0.0016 Angstrom

<001> FWHM= 0.068 degrees (2theta)

<002> FWHM= 0.075 degrees

<003> FWHM= 0.069 degrees

<103> FWHM= 0.107 degrees

<203> FWHM= 0.082 degrees

rocking curves

<001> FWHM= 0.031 degrees (theta)

<002> FWHM= 0.035 degrees

<003> FWHM= -     degrees

<103> FWHM= 0.034 degrees

<203> FWHM= -     degrees

film

h  k  l 2th-meas  2th-cal   diff.

0  0  1  23.3230  23.3317  -0.0087

0  0  2  47.7040  47.7080  -0.0040

0  0  3  74.6790  74.6897  -0.0107

1  0  3  79.2620  79.2626  -0.0006

2  0  3  92.6900  92.6887   0.0013

a=  3.9071 +/-  0.0028 Angstrom, zero-offset=  -0.0045

c=  3.8095 +/-  0.0009 Angstrom

v= 58.1544 +/-  0.0597 A^3

<001> FWHM= 0.373 degrees (2theta)

<002> FWHM= 0.421 degrees

<003> FWHM= 0.514 degrees

<103> FWHM= 0.286 degrees

<203> FWHM= 0.245 degrees

rocking curves

<001> FWHM= 0.043 degrees (theta)

<002> FWHM= 0.044 degrees

<003> FWHM= -     degrees

<103> FWHM= 0.054 degrees

<203> FWHM= =     degrees

L408 (LaCa)MnO3 on SrTiO3 (Ivan) layer thickness =     45 nm

Substrate

h  k  l 2th-meas  2th-cal   diff.

0  0  1  22.7620  22.7462   0.0158

0  0  2  46.4960  46.4564   0.0396

0  0  3  72.5630  72.5400   0.0230

1  0  3  77.1830  77.1578   0.0252

2  0  3  90.6550  90.6333   0.0217

a=  3.9062 +/-  0.0004 Angstrom,

<001> FWHM= 0.051 degrees (2theta)

<002> FWHM= 0.067 degrees

<003> FWHM= 0.070 degrees

<103> FWHM= 0.074 degrees

<203> FWHM= 0.079 degrees

rocking curves

<001> FWHM= 0.030 degrees (theta)

<002> FWHM= 0.030 degrees

<003> FWHM= 0.031 degrees

<103> FWHM= 0.026 degrees

<203> FWHM= 0.025 degrees

film

h  k  l 2th-meas  2th-cal   diff.

0  0  1  23.3620  23.3400   0.0220

0  0  2  47.7640  47.7258   0.0382

1  0  2  53.5340  53.4916   0.0424

0  0  3  74.7650  74.7204   0.0446

1  0  3  79.2970  79.2928   0.0042

2  0  3  92.7170  92.7183  -0.0013

a=  3.9071 +/-  0.0068 Angstrom,

c=  3.8082 +/-  0.0005 Angstrom

<001> FWHM= 0.248 degrees (2theta)

<002> FWHM= 0.280 degrees

<003> FWHM= 0.377 degrees

<102> FWHM= 0.155 degrees

<103> FWHM= 0.397 degrees

<203> FWHM= 0.472 degrees

rocking curves

<001> FWHM= 0.033 degrees (theta)

<002> FWHM= 0.044 degrees

<003> FWHM= 0.187 degrees

<102> FWHM= 0.099 degrees

<103> FWHM= 0.155 degrees

<203> FWHM= 0.178 degrees

L414 (LaCa)MnO3 on SrTiO3 (Ivan)

substrate

h  k  l 2th-meas  2th-cal   diff.

0  0  1  22.7810  22.7410   0.0400

0  0  2  46.5160  46.4453   0.0707

0  0  3  72.5870  72.5210   0.0660

1  0  3  77.1770  77.1372   0.0398

2  0  3  90.6510  90.6071   0.0439

a=  3.9071 +/-  0.0007 Angstrom,

<001> FWHM= 0.060 degrees (2theta)

<002> FWHM= 0.065 degrees

<003> FWHM= 0.079 degrees

<103> FWHM= 0.088 degrees

rocking curves

<001> FWHM= 0.050 degrees (theta)

<002> FWHM= 0.047 degrees

<003> FWHM= 0.044 degrees

<103> FWHM= 0.055 degrees

film

h  k  l 2th-meas  2th-cal   diff.

0  0  1  23.3970  23.3827   0.0143

0  0  2  47.8230  47.8172   0.0058

1  0  2  53.6200  53.6025   0.0175

0  0  3  74.8850  74.8782   0.0068

1  0  3  79.4630  79.4696  -0.0066

a=  3.8977 +/-  0.0076 Angstrom,

c=  3.8013 +/-  0.0006 Angstrom

<001> FWHM= 0.227 degrees (2theta)

<002> FWHM= 0.294 degrees

<003> FWHM= 0.447 degrees

<102> FWHM= 0.280 degrees

<103> FWHM= 0.402 degrees

rocking curves

<001> FWHM= 0.061 degrees (theta)

<002> FWHM= 0.092 degrees

<003> FWHM= 0.110 degrees

<102> FWHM= 0.190 degrees

<103> FWHM= 0.166 degrees

<203> FWHM= 0.237 degrees

L420 (LaCa)MnO3 on SrTiO3 (Ivan) d=25.6 nm

Substrate

h  k  l 2th-meas  2th-cal   diff.

0  0  1  22.7840  22.7377   0.0463

0  0  2  46.5040  46.4383   0.0657

0  0  3  72.5730  72.5091   0.0639

1  0  3  77.1650  77.1242   0.0408

2  0  3  90.6450  90.5908   0.0542

a=  3.9077 +/-  0.0007 Angstrom,

<001> FWHM= 0.064 degrees (2theta)

<002> FWHM= 0.063 degrees

<003> FWHM= 0.078 degrees

<103> FWHM= 0.077 degrees

<203> FWHM= 0.087 degrees

rocking curves

<001> FWHM= 0.063 degrees (theta)

<002> FWHM= 0.055 degrees

<003> FWHM= 0.000 degrees

<103> FWHM= 0.000 degrees

<203> FWHM= 0.000 degrees

film

h  k  l 2th-meas  2th-cal   diff.

0  0  1  23.2210  23.2547  -0.0337

0  0  2  47.5590  47.5431   0.0159

1  0  2  53.4160  53.3616   0.0544

0  0  3  74.4360  74.4054   0.0306

1  0  3  79.0020  79.0147  -0.0127

2  0  3  92.5040  92.5368  -0.0328

a=  3.8938 +/-  0.0089 Angstrom,

c=  3.8220 +/-  0.0010 Angstrom

<001> FWHM= 0.277 degrees (2theta)

<002> FWHM= 0.421 degrees

<003> FWHM= 0.583 degrees

<102> FWHM= 0.332 degrees

<103> FWHM= 0.375 degrees

<203> FWHM= 0.000 degrees

rocking curves

<001> FWHM= 0.121 degrees (theta)

<002> FWHM= 0.092 degrees

<003> FWHM= 0.000 degrees

<103> FWHM= 0.000 degrees

<203> FWHM= 0.000 degrees

L425 (LaCa)MnO3 on SrTiO3

Substrate

h  k  l 2th-meas  2th-cal   diff.

0  0  1  22.7570  22.7477   0.0093

0  0  2  46.4780  46.4597   0.0183

0  0  3  72.5490  72.5456   0.0034

1  0  3  77.1800  77.1639   0.0161

2  0  3  90.6450  90.6410   0.0040

a=  3.9060 +/-  0.0007 Angstrom,

<001> FWHM= 0.048 degrees (2theta)

<002> FWHM= 0.064 degrees

<003> FWHM= 0.000 degrees

<103> FWHM= 0.077 degrees

<203> FWHM= 0.085 degrees

rocking curves

<001> FWHM= 0.071 degrees (theta)

<002> FWHM= 0.066 degrees

<003> FWHM= 0.060 degrees

<103> FWHM= 0.056 degrees

<203> FWHM= 0.047	 degrees

film

h  k  l 2th-meas  2th-cal   diff.

0  0  1  23.3000  23.3153  -0.0153

0  0  2  47.5430  47.6728  -0.1298

1  0  2  53.4760  53.4543   0.0217

0  0  3  74.5540  74.6290  -0.0750

1  0  3  79.2160  79.2124   0.0036

2  0  3  92.6310  92.6670  -0.0360

a=  3.9031 +/-  0.0235 Angstrom,

c=  3.8122 +/-  0.0027 Angstrom

<001> FWHM= -     degrees (2theta)

<002> FWHM= 0.743 degrees

<003> FWHM= 0.828 degrees

<102> FWHM= 0.156 degrees

<103> FWHM= 0.328 degrees

<203> FWHM= 0.215 degrees

rocking curves

<001> FWHM= 0.069 degrees (theta)

<002> FWHM= 0.067 degrees

<003> FWHM= 0.060 degrees

<102> FWHM= 0.080 degrees

<103> FWHM= 0.074 degrees

<203> FWHM= 0.062 degrees

L427 (LaCa)MnO3 on SrTiO3

Substrate

h  k  l 2th-meas  2th-cal   diff.

0  0  1  22.7550  22.7397   0.0153

0  0  2  46.4720  46.4426   0.0294

0  0  3  72.5440  72.5164   0.0276

1  0  3  77.1410  77.1322   0.0088

2  0  3  90.6090  90.6008   0.0082

a=  3.9073 +/-  0.0009 Angstrom

<001> FWHM= 0.052 degrees (2theta)

<002> FWHM= 0.070 degrees

<003> FWHM= 0.088 degrees

<103> FWHM= 0.085 degrees

<203> FWHM= 0.092 degrees

rocking curves

<001> FWHM= 0.080 degrees (theta)

<002> FWHM= 0.059 degrees

<003> FWHM= 0.045 degrees

<103> FWHM= 0.059 degrees

<203> FWHM= 0.065 degrees

film

h  k  l 2th-meas  2th-cal   diff.

0  0  1  23.1310  23.2370  -0.1060

0  0  2  47.3900  47.5051  -0.1151

0  0  3  74.2660  74.3399  -0.0739

1  0  3  78.9190  78.9357  -0.0167

2  0  3  92.4100  92.4157  -0.0057

a=  3.9001 +/-  0.0166 Angstrom,

c=  3.8248 +/-  0.0011 Angstrom

<001> FWHM= -     degrees (2theta)

<002> FWHM= 0.447 degrees

<003> FWHM= 0.588 degrees

<103> FWHM= 0.424 degrees

<203> FWHM= 0.567 degrees

rocking curves

<001> FWHM= 0.104 degrees (theta)

<002> FWHM= 0.128 degrees

<003> FWHM= 0.161 degrees

<103> FWHM= 0.170 degrees

<203> FWHM= 0.200 degrees

L432 (LaCa)MnO3 on SrTiO3

Substrate

h  k  l 2th-meas  2th-cal   diff.

0  0  1  22.7700  22.7434   0.0266

0  0  2  46.4930  46.4505   0.0425

0  0  3  72.5580  72.5299   0.0281

1  0  3  77.1650  77.1469   0.0182

2  0  3  90.6340  90.6194   0.0146

a=  3.9067 +/-  0.0009 Angstrom,

<001> FWHM= 0.056 degrees (2theta)

<002> FWHM= 0.067 degrees

<003> FWHM= 0.073 degrees

<103> FWHM= 0.071 degrees

<203> FWHM= 0.078 degrees

rocking curves

<001> FWHM= 0.037 degrees (theta)

<002> FWHM= 0.036 degrees

<003> FWHM= 0.040 degrees

<103> FWHM= 0.040 degrees

<203> FWHM= 0.037 degrees

film

h  k  l 2th-meas  2th-cal   diff.

0  0  1  23.2030  23.3045  -0.1015

0  0  2  47.6600  47.6497   0.0103

1  0  2  53.4830  53.4711   0.0119

0  0  3  74.5850  74.5891  -0.0041

1  0  3  79.1990  79.2044  -0.0054

2  0  3  92.7360  92.7509  -0.0149

a=  3.8898 +/-  0.0024 Angstrom,

c=  3.8139 +/-  0.0005 Angstrom

<001> FWHM= -     degrees (2theta)

<002> FWHM= 0.574 degrees

<102> FWHM= 0.150 degrees

<003> FWHM= 0.738 degrees

<103> FWHM= 0.222 degrees

<203> FWHM= 0.211 degrees

rocking curves

<001> FWHM= 0.043 degrees (theta)

<002> FWHM= 0.041 degrees

<102> FWHM= 0.073 degrees

<003> FWHM= 0.040 degrees

<103> FWHM= 0.050 degrees

<203> FWHM= 0.057 degrees

L437 (LaCa)MnO3 on SrTiO3 (before annealing)

Substrate

h  k  l 2th-meas  2th-cal   diff.

0  0  1  22.7750  22.7461   0.0289

0  0  2  46.4910  46.4563   0.0347

0  0  3  72.5660  72.5398   0.0262

1  0  3  77.1730  77.1576   0.0154

2  0  3  90.6470  90.6331   0.0139

a=  3.9063 +/-  0.0008 Angstrom,

<001> FWHM= 0.059 degrees (2theta)

<002> FWHM= 0.070 degrees

<003> FWHM= 0.079 degrees

<103> FWHM= 0.084 degrees

<203> FWHM= 0.092 degrees

rocking curves

<001> FWHM= 0.056 degrees (theta)

<002> FWHM= 0.055 degrees

<003> FWHM= 0.045 degrees

<103> FWHM= 0.000 degrees

<203> FWHM= 0.073 degrees

film

h  k  l 2th-meas  2th-cal   diff.

0  0  1  23.3910  23.3925  -0.0015

0  0  2  47.8120  47.8383  -0.0263

0  0  3  74.8520  74.9147  -0.0627

1  0  3  79.4750  79.4854  -0.0104

2  0  3  92.9130  92.9135  -0.0005

a=  3.9063 +/-  0.0153 Angstrom,

c=  3.7998 +/-  0.0010 Angstrom

<001> FWHM= 0.214 degrees (2theta)

<002> FWHM= 0.262 degrees

<003> FWHM= 0.402 degrees

<103> FWHM= 0.352 degrees

<203> FWHM= 0.292 degrees

rocking curves

<001> FWHM= 0.056 degrees (theta)

<002> FWHM= 0.059 degrees

<003> FWHM= 0.096 degrees

<103> FWHM= 0.000 degrees

<203> FWHM= 0.124 degrees

L437 (LaCa)MnO3 on SrTiO3 (after annealing 840 C 10 hrs 1 bar O2)

Substrate

h  k  l 2th-meas  2th-cal   diff.

0  0  1  22.7710  22.7456   0.0254

0  0  2  46.4940  46.4551   0.0389

1  0  3  77.1770  77.1554   0.0216

2  0  3  90.6590  90.6303   0.0287

a=  3.9063 +/-  0.0013 Angstrom,

<001> FWHM= 0.059 degrees (2theta)

<002> FWHM= 0.072 degrees

<103> FWHM= 0.056 degrees

<203> FWHM= 0.091 degrees

rocking curves

<001> FWHM= 0.056 degrees (theta)

<002> FWHM= 0.051 degrees

<103> FWHM= 0.047 degrees

<203> FWHM= 0.048 degrees

film

h  k  l 2th-meas  2th-cal   diff.

0  0  1  23.2800  23.2783   0.0017

0  0  2  47.5980  47.5936   0.0044

1  0  3  79.1090  79.1078   0.0012

2  0  3  92.6510  92.6507   0.0003

a=  3.8905 +/-  0.0018 Angstrom,

c=  3.8181 +/-  0.0005 Angstrom

<001> FWHM= 0.239 degrees (2theta)

<002> FWHM= 0.413 degrees

<103> FWHM= 0.590 degrees

<203> FWHM= 0.577 degrees

rocking curves

<001> FWHM= 0.082 degrees (theta)

<002> FWHM= 0.224 degrees

<103> FWHM= 0.234 degrees

<203> FWHM= 0.276 degrees

L438 (LaCa)MnO3 on SrTiO3 (before annealing) d=8.9 nm

Substrate

h  k  l 2th-meas  2th-cal   diff.

0  0  1  22.7830  22.7462   0.0368

0  0  2  46.4940  46.4564   0.0376

0  0  3  72.5690  72.5400   0.0290

1  0  3  77.1860  77.1578   0.0282

2  0  3  90.6650  90.6333   0.0317

a=  3.9062 +/-  0.0002 Angstrom,

<001> FWHM= 0.062 degrees (2theta)

<002> FWHM= 0.067 degrees

<003> FWHM= 0.079 degrees

<103> FWHM= 0.079 degrees

<203> FWHM= 0.086 degrees

rocking curves

<002> FWHM= 0.057 degrees (theta)

<003> FWHM= 0.053 degrees

<103> FWHM= 0.060 degrees

<203> FWHM= 0.071 degrees

film

h  k  l 2th-meas  2th-cal   diff.

0  0  2  47.4780  47.4403   0.0377

1  0  3  78.8820  78.8609   0.0211

2  0  3  92.4610  92.4445   0.0165

a=  3.8853 +/-  0.0032 Angstrom,

c=  3.8298 +/-  0.0008 Angstrom

<002> FWHM= 0.737 degrees (2theta)

<103> FWHM= 0.343 degrees

<203> FWHM= -     degrees

rocking curves

<001> FWHM= 0.000 degrees (theta)

<002> FWHM= 0.054 degrees

<003> FWHM= 0.000 degrees

<103> FWHM= 0.068 degrees

<203> FWHM= -     degrees

L441 (LaCa)MnO3 on SrTiO3 d=5.0 nm

Substrate

h  k  l 2th-meas  2th-cal   diff.

1  0  3  77.1710  77.1639   0.0071

2  0  3  90.6380  90.6410  -0.0030

a=  3.9060 +/-  0.0010 Angstrom

<103> FWHM= 0.080 degrees (2theta)

<203> FWHM= 0.000 degrees

rocking curves

<103> FWHM= 0.071 degrees (theta)

<203> FWHM= 0.000 degrees

film

h  k  l 2th-meas  2th-cal   diff.

1  0  3  78.7680  78.7680  -0.0000

2  0  3  92.1680  92.1680  -0.0000

a=  3.9122 +/-  0.0000 Angstrom, (should be 3.906 A)

c=  3.8311 +/-  0.0000 Angstrom

<103> FWHM= 0.390 degrees (2theta)

<203> FWHM= -     degrees

rocking curves

<103> FWHM= 0.100 degrees (theta)

<203> FWHM= -     degrees

L446 (LaCa)MnO3 on SrTiO3 d=8.5 nm

Substrate

h  k  l 2th-meas  2th-cal   diff.

0  0  1  22.7870  22.7522   0.0348

0  0  2  46.5070  46.4692   0.0378

0  0  3  72.5810  72.5620   0.0191

1  0  3  77.1980  77.1817   0.0163

2  0  3  90.6830  90.6636   0.0194

a=  3.9052 +/-  0.0010 Angstrom,

<001> FWHM= 0.047 degrees (2theta)

<002> FWHM= 0.062 degrees

<003> FWHM= 0.068 degrees

<103> FWHM= 0.080 degrees

<203> FWHM= 0.094 degrees

rocking curves

<001> FWHM= -     degrees (theta)

<002> FWHM= 0.054 degrees

<003> FWHM= -     degrees

<103> FWHM= 0.064 degrees

<203> FWHM= 0.080 degrees

film

h  k  l 2th-meas  2th-cal   diff.

0  0  2  47.5170  47.5257  -0.0087

1  0  3  79.0470  79.0470   0.0000

2  0  3  92.7530  92.7506   0.0024

a=  3.8677 +/-  0.0010 Angstrom,

c=  3.8233 +/-  0.0008 Angstrom

<001> FWHM= -     degrees (2theta)

<002> FWHM= 0.882 degrees

<003> FWHM= -     degrees

<103> FWHM= 0.000 degrees

<203> FWHM= 0.265 degrees

rocking curves

<001> FWHM= -     degrees (theta)

<002> FWHM= 0.044 degrees

<003> FWHM= -     degrees

<103> FWHM= 0.066 degrees

<203> FWHM= 0.097 degrees

L457 (LaCa)MnO3 on SrTiO3 d=10.9 nm

Substrate

h  k  l 2th-meas  2th-cal   diff.

0  0  1  22.7740  22.7480   0.0260

0  0  2  46.4990  46.4602   0.0388

0  0  3  72.5700  72.5465   0.0235

1  0  3  77.1750  77.1649   0.0101

a=  3.9059 +/-  0.0007 Angstrom, zero-offset=   0.0246

v= 59.5905 +/-  0.0172 A^3

<002> FWHM= 0.076 degrees (2theta)

<103> FWHM= 0.097 degrees

film

h  k  l 2th-meas  2th-cal   diff.

0  0  2  47.6250  47.6250   0.0000

1  0  3  79.1250  79.1250   0.0000

a=  3.9059 +/-  0.0000 Angstrom,

c=  3.8158 +/-  0.0000 Angstrom

<002> FWHM= 0.727 degrees (2theta)

<103> FWHM= 0.447 degrees

L461 (LaCa)MnO3 on SrTiO3 d=5.0 nm

Substrate

h  k  l 2th-meas  2th-cal   diff.

0  0  2  46.4930  46.4596   0.0334

1  0  3  77.1810  77.1638   0.0172

2  0  3  90.6670  90.6409   0.0261

a=  3.9060 +/-  0.0023 Angstrom, zero-offset=   0.0255

v= 59.5927 +/-  0.0617 A^3

<002> FWHM= 0.072 degrees (2theta)

<103> FWHM= 0.081 degrees

<203> FWHM= 0.086 degrees

h  k  l 2th-meas  2th-cal   diff.

0  0  2  47.6400  47.6416  -0.0016

1  0  3  79.1400  79.1406  -0.0006

2  0  3  92.5400  92.5403  -0.0003

a=  3.9113 +/-  0.0000 Angstrom, (should be max 3.9060 A)

c=  3.8145 +/-  0.0000 Angstrom

<002> FWHM= -     degrees (2theta)

<103> FWHM= 0.324 degrees

<203> FWHM= 0.251 degrees

template

Substrate

<001> FWHM= 0.000 degrees (2theta)

<002> FWHM= 0.000 degrees

<003> FWHM= 0.000 degrees

<103> FWHM= 0.000 degrees

<203> FWHM= 0.000 degrees

rocking curves

<001> FWHM= 0.000 degrees (theta)

<002> FWHM= 0.000 degrees

<003> FWHM= 0.000 degrees

<103> FWHM= 0.000 degrees

<203> FWHM= 0.000 degrees

film

<001> FWHM= 0.000 degrees (2theta)

<002> FWHM= 0.000 degrees

<003> FWHM= 0.000 degrees

<103> FWHM= 0.000 degrees

<203> FWHM= 0.000 degrees

rocking curves

<001> FWHM= 0.000 degrees (theta)

<002> FWHM= 0.000 degrees

<003> FWHM= 0.000 degrees

<103> FWHM= 0.000 degrees

<203> FWHM= 0.000 degrees